Supplementary Materials

Synthesis of a Slow-Release Fertilizer Composite Based on Microcrystalline Cellulose from Coconut Husk Waste

Vicka Andinia*, Yoravika Dwiwibanggaa, Safniyetib, Nasywa Az Zahraa, Ulfah Anisc, Mega Elfiaa

a Department of Chemistry, Faculty of Sciences and Mathematics, The University of Bengkulu, Bengkulu, Indonesia

b Department of Biology, Faculty of Sciences and Mathematics, The University of Bengkulu, Bengkulu, Indonesia

c Department of Agricultural Technology, Faculty of Agriculture, The University of Bengkulu, Bengkulu, Indonesia

E-mail addresses: vandini@unib.ac.id*, ydwiwibangga@unib.ac.id, ssafniyeti@unib.ac.id, nzahraaa6@gmail.com, ulfahanis@unib.ac.id, megaelfia@unib.ac.id

Corresponding author: vandini@unib.ac.id

This Supplementary Materials document provides photographic documentation of the sample preparation and synthesis processes, EDX spectrum of elemental composition, and FTIR peak table, to support the characterization results presented in the main manuscript.

Figure S1. Freshly cleaned and sun-dried coir

Figure S2. Ground coconut coir powder

Figure S3. Sieved powder of coconut coir (18 mesh).

Figure S4. Microcrystalline cellulose (MCC) was obtained from coconut coir after sequential extraction and acid hydrolysis.

Figure S5. Polydihydroxymethylurea potassium phosphate (PDMU–K) is obtained after polycondensation and thermal curing.

Figure S6. Microcrystalline cellulose-g-poly(maleic acid)/polyhydroxymethylurea potassium phosphate (MCC-g-PMA/PDMU–KP) copolymer synthesized using citric acid as an interaction agent.

Figure S7. EDX spectrum of elemental composition of coconut husk.

Figure S8. EDX spectrum of elemental composition of MCC.

Figure S9. EDX spectrum of elemental composition of PDMU–KP.

Figure S10. EDX spectrum of elemental composition of MCC-g-PMA/PDMU–KP.

Table S1. FTIR peak assignments of coconut husk

| Wavenumber (cm-1) | Functional Groups |
| --- | --- |
| 3400–3200 | O–H stretching |
| 2922 | aliphatic C–H stretching |
| 1732 | C=O stretching |
| 1609 and 1518 | aromatic C=C skeletal |
| 1247 | C–O stretching |
| 1050–1030 | C–O–C and C–O stretching |

Table S2. FTIR peak assignments of MCC

| Wavenumber (cm-1) | Functional Groups |
| --- | --- |
| 3400–3200 | O–H stretching |
| 2889 | aliphatic C–H stretching |
| 1724 | C=O stretching |
| 1625 and 1592 | aromatic C=C skeletal |
| 1430 | CH2 bending |
| 1370 | C–H bending |
| 1321 | CH2 wagging |
| 1157 | C–O–C stretching |
| 1026 | C–O stretching |
| 895 | C–H out-of-plane |

Table S3. FTIR peak assignments of PDMU–KP

| Wavenumber (cm-1) | Functional Groups |
| --- | --- |
| 3440 and 3325 | O–H and N–H stretching |
| 2955 | aliphatic C–H stretching |
| 1642 | C=O stretching |
| 1551 | N–H bending + C–N stretching |
| 1346 | C–N stretching |
| 1264 | P=O stretching |
| 1133 | P–O stretching |
| 1026 | C–O–P stretching |
| 895 | –P–O bending |

Table S4. FTIR peak assignments of MCC-g-PMA/PDMU–KP composite.

| Wavenumber (cm-1) | Functional Groups |
| --- | --- |
| 3400–3200 | O–H/N–H stretching |
| 3300–2500 | O–H stretching |
| 1720–1710 | C=O stretching |
| 1642 | C=O stretching |
| 1568 | N–H bending + C–N stretching |
| 1477 | CH2 bending |
| 1149–870 | P–O, P=O, C–O–C stretching |