Journal : Reaktor

Manuscript ID :

Title: Cracking of Methyl Ester from Used-Cooking Oil Using Ni-Impregnated Active Charcoal Catalyst

There are some comments from the reviewer and how the authors have responded:

Reviewer 1

| Reviewer’s Comments | Author’s Comments |
| --- | --- |
| pls recheck English: palm, Nickel (nickel), etc | Some changes have been made in the manuscript |
| abstract: The methyl ester was produced by transesterification of | The methyl ester was produced by transesterification of used cooking oil and methanol (has been added in the manuscript) |
| abstract: pls add the main results. | The main results have been added |
| intro: pls update with new refs | We have updated the references as follows: Kouzu et al, 2020 Menshhein et al., 2019 Kayode & Hart, 2017 |
| exp section: this is not impregnation. pls see an example of impregnation: https://www.sciencedirect.com/science/article/pii/S0016236121001411 | We are unable to get access of full paper for article in the link given by the reviewer. We have checked in other journals and what we have done is similar to (Kiani et al., 2021) https://www.sciencedirect.com/science/article/abs/pii/S0925963520307329 |
| exp section, last para: "Gravimetric analysis was used to determine percent of conversion of each cracking products, total conversion, percent residu and conversion ratio using equations" - conversion is for reactant, not product - only show two equations | We have change the term into “yields” There are 2 equations in this paragraph |
| cooking oil was 0.9534 g/cm3 and that of methyl ester was 0.9154 g/cm3). Cracking process breaks double[Ma1] bonds and evaporates some carbon compound leading to lower density of the product. However, the densities of OLFs were still slighty higher than the density of B20 (0.88 g/cm3) [Ma2] which composed of 20% methyl ester and 80% commercial solar [Ma1]pls support with your data found [Ma2]density of the products are higher than methyl ester (in between. look like not cracking, still have high density. | GCMS analysis showed that the methyl ester contained 49.12% C19 compounds and 32.44% C17 compound. Catalytic cracking of the methyl ester changed the composition to 47.55% C17 carbon compund and 40.35% C17/C19 There was a little decrease in the length of carbon chain. |
| Please support the data with the GCMS | The GCMS for OLF from catalytic cracking of methyl ester have been added The GCMS for methyl ester have been previously published (Alfernando et al., 2019) and cited in the manuscript |